GENERAL

SECTION INCLUDES

Noise-reducing recycled rubber impact insulation systems

Adhesives

RELATED SECTIONS

Concrete Substrate

Plywood Substrate

Tile, Carpet, Wood

Noise Control and Vibration Isolation

REFERENCES

U.S. Department of Housing and Urban Development (HUD): Guide to Airborne, Impact, and Structure Borne Noise Control in Multifamily Dwellings.

American Society for Testing and Materials (ASTM)

ASTM E492 Standard Test Method for Laboratory Measurement of Impact Sound Transmission Through Floor-Ceiling Assemblies Using the Tapping Machine

ASTM D5116 Standard Guide for small-scale environmental chamber determinations of Organic Emissions for Indoor Material/ Products

ASTM C627 Standard Test Method of Evaluating Ceramic Tile Installation Systems using the Robinson Type Floor Test

ASTM E1007 Standard Test Method for Field Measurement of Tapping Machine Impact Sound Transmission through Floor-Ceiling assemblies and Associated support structures

ASTM E2179 Standard Test Method for Laboratory Measurement of the Effectiveness of Floor Coverings in Reducing Impact Sound Transmission through Concrete Floors

ASTM E90 E2179 Standard Test Method for Laboratory Measurement of Airborne Sound Transmission loss of Building Partitions and Elements

Leadership in Energy and Environmental Design -LEED®

LEED is an internationally recognized green building certification system, providing third-party verification that a building or community was designed and built using strategies aimed at improving performance across all the metrics that matter most: energy savings, water efficiency, CO2 emissions reduction, improved indoor environmental quality, and stewardship of resources and sensitivity to their impacts.

SYSTEM DESCRIPTION

Performance Requirements: Provide recycled rubber resilient underlayment padding, which has been manufactured and installed to maintain performance criteria stated by manufacturer without defects, damage or failure.

SUBMITTALS

Submit under provisions of Section 01300.

Product Data:  Manufacturer's data sheets on each product to be used, including:

Preparation instructions and recommendations.

Storage and handling requirements and recommendations.

Installation methods.

LEED Documentation of how the requirement for credit will be met.

Selection Samples:  For each finish product specified, two complete sets of color chips representing manufacturer's full range of available colors and patterns.

Verification Samples:  For each finish product specified, two samples, minimum size 6 inches (150 mm) square, representing actual product, color, and patterns.

QUALITY ASSURANCE

Manufacturer Qualifications: The manufacturer shall be a firm with a minimum of two years of successful experience in manufacture of products with similar requirements.

Installer Qualifications: The installer shall be a firm with a minimum of two years of successful experience in installation of products with similar requirements.

Mock-Up:  Provide a mock-up for evaluation of surface preparation techniques and application workmanship.

Finish areas designated by Architect.

Do not proceed with remaining work until workmanship, color, and sheen are approved by Architect.

Refinish mock-up area as required to produce acceptable work.

DELIVERY, STORAGE, AND HANDLING

Store products in manufacturer's unopened packaging until ready for installation.

Store and dispose of solvent-based materials, and materials used with solvent-based materials, in accordance with requirements of local authorities having jurisdiction.

PROJECT CONDITIONS

Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results.  Do not install products under environmental conditions outside manufacturer's absolute limits.

PRODUCTS

MANUFACTURER:

Acceptable Manufacturer:
Regupol America, LLC 
11 Ritter Way
Lebanon, PA 17042
Toll Free Tel: (800) 537-8737
Tel: (717) 675-2198.  
Fax: (717) 675-2199
Email: bmd@regupol.com
Web: http:// www.Regupol.com.

Substitutions:  Not permitted.

Requests for substitutions will be considered in accordance with provisions of Section 01600.

PRODUCT

REGUPOL sonus curve 8 Recycled rubber Impact Sound Insulation

Material:

Made from 100% recycled SBR (Styrene-Butadiene Rubber) tire rubber. Sonus curve 8 is a dimpled resilient rubber-based mat that can be applied under gypsum or full weight concrete.

Physical Characteristics:

8mm thick with 4mm dimple

48” inches by 25 ft rolls.

Material Weight .75 lb/ft²

Impact Insulation Class

16” open web truss assembly w/gypsum topping (IIC 57) STC (64)

8mm SonusWave, ¾” plywood, nail down hardwood

REGUPOL sonus iso-strips rubber Perimeter Isolation Strip

Material:

Made from 100% recycled SBR (Styrene-Butadiene Rubber) tire rubber.

Physical Characteristics:

4” x 5’ x ¼” thick rubber isolation strips to be installed around perimeter or any protruding object in room to avoid sound flanking paths

4 Mil Polyethylene Film (not required with plywood or eng. hardwood)

Material:

4 mil Polyethylene sheeting to be installed over sonus curve to prevent leakage of lightweight gypsum or concrete topping

EXECUTION

EXAMINATION

Do not begin installation until substrates have been properly prepared.

If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

PREPARATION

Clean surfaces thoroughly prior to installation.

Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

INSTALLATION

Install in accordance with manufacturer's instructions.

PROTECTION

Protect installed products until completion of project.

Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION